## Slide 1
Dezső Sima
Evolution of Intel’s
transistor technology
45 nm – 14 nm
September 2015
Vers. 1.1

## Slide 2
Contents
1. Overview of the evolution of Intel’s basic microarchitectures
2. The high-k + metal gate transistor
3. The 22 nm 3D Tri-Gate transistor
4. The 14 nm 3D Tri-Gate transistor

## Slide 3
1. Overview of the evolution of Intel’s basic microarchitectures
Notes: 3

## Slide 4: 1. Overview of the evolution of Intel’s basic microarchitectures-1
1. Overview of the evolution of Intel’s basic microarchitectures (Based on [1])
Figure 1.1: Intel’s Tick-Tock development model (Based on [1])
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 5: 1. Overview of the evolution of Intel’s basic microarchitectures-2
Evolution of Intel’s process technologies [82]
2014
High K +
Metalgate
Tri Gate
1. gen.
Tri Gate
2. gen.
New transistor
structures
Penryn
Ivy Bridge
Broadwell
Related
proc. family
2016?

## Slide 6: 1. Overview of the evolution of Intel’s basic microarchitectures-3
Intel’s relative yield trends of their 14 nm technology vs. their 22 nm technology [154]

## Slide 7: 1. Overview of the evolution of Intel’s basic microarchitectures-4
The last two technology transitions have signaled that our cadence today is closer to 2.5 years than two“ [180].
On Intel’s Q2 2015 earnings conference call, on July 16 2015, Krzanich: in the second half of 2017, we expect to launch our first 10-nanometer product, code named Cannonlake.
The cadence of Intel’s technology transitions [179]
2000
2002
2004
2006
2008
2010
2012
2014
2016
2018
200
180
160
140
120
100
80
60
40
0
20
180 nm
130 nm
90 nm
65 nm
45 nm
32 nm
22 nm
14 nm
10 nm
Pentium 4
Northwood
Pentium 4
Prescott
Pentium 4
Cedar Mill
Penryn
Westmere
Ivy Bridge
Broadwell
Pentium 4
Willamette
Cannonlake
01/02
02/04
11/07
01/10
04/12
09/14
11/00
2H/17
01/06
nm

## Slide 8: 1. Overview of the evolution of Intel’s basic microarchitectures-5
Intel’s lead in IC technology according to [154]
Source: Intel 08/2014
Others:
TMSC (Taiwan)
Globalfoundries (Abu Dhabi)
( IBM Microelectronic)
Samsung Semiconductor
(South Korea)

## Slide 9
2. The high-k + metal gate transistor
Notes: 9

## Slide 10: 2. The high-k + metal gate transistor-1
Introduced along with the Penryn family of processors in 2007.
Figure: Intel’s Tick-Tock development model (Based on [1])
2. The high-k + metal gate transistor
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 11: 2. The high-k + metal gate transistor-2
Figure 3.1.1: Dynamic and static power dissipation trends in chips [21]
Sub-threshold =
Source-Drain
The need to introduce new transistor design [21]

## Slide 12: 2. The high-k + metal gate transistor-3
Structure of the high-k + metal gate transistors [23]

## Slide 13: 2. The high-k + metal gate transistor-4
Benefits of the high-k + metal gate transistors [23], [24]

## Slide 14
3. The 22 nm 3D Tri-Gate transistor
Notes: 14

## Slide 15: 3. The 22 nm 3D Tri-Gate transistor-1
Introduced along with the Ivy Bridge family of processors in 2012.
Figure: Intel’s Tick-Tock development model (Based on [1])
3. The 22 nm 3D Tri-Gate transistor-1
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 16: 3. The 22 nm 3D Tri-Gate transistor-2
The traditional planar transistor [82]

## Slide 17: 3. The 22 nm 3D Tri-Gate transistor-3
The 22 nm 3D Tri-Gate transistor-2 [82]
The designation “tri-gate” originates from the fact that now the gate has three sides.
fin

## Slide 18: 3. The 22 nm 3D Tri-Gate transistor-4
The 22 nm Tri-Gate transistor-3 [82]

## Slide 19: 3. The 22 nm 3D Tri-Gate transistor-5
Switching characteristics of the traditional planar and tri-gate transistors [82]

## Slide 20: 3. The 22 nm 3D Tri-Gate transistor-6
Gate delay of the traditional planar and tri-gate transistors [82]
Gate delay: time difference between output signal and input signal of a gate (n x ps)

## Slide 21: 3. The 22 nm 3D Tri-Gate transistor-7
Intel’s 22 nm manufacturing fabs [82]

## Slide 22: 3. The 22 nm 3D Tri-Gate transistor-8
22 nm Ivy Bridge chips on a 300 mm wafer [82]

## Slide 23
4. The 14 nm 3D Tri-Gate transistor
Notes: 23

## Slide 24: 4. The 14 nm 3D Tri-Gate transistor-1
Figure: Intel’s Tick-Tock development model (Based on [1])
4. The 14 nm 3D Tri-Gate transistor-1
Introduced along with the Broadwell family of processors in 2014
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 25: 4. The 14 nm 3D Tri-Gate transistor-2
14 nm 2 generation Tri-gate transistors with fin improvement [154]

## Slide 26: 4. The 14 nm 3D Tri-Gate transistor-3
14 nm Broadwell SOC yield trend [154]

## Slide 27: 4. The 14 nm 3D Tri-Gate transistor-4
Benefits of reducing the feature size [154]

## Slide 28: 4. The 14 nm 3D Tri-Gate transistor-4
Leakage power vs clock speed for smaller feature sizes [154]
fc > Vc
Vc > Il > Ds

## Slide 29: 4. The 14 nm 3D Tri-Gate transistor-5
Leakage power vs. clock speed for smaller feature sizes in different product sectors [154]