## Slide 1
Dezső Sima
Evolution of transistor technology
Sept. 2016
Vers. 2.1

## Slide 2
Contents
1. Introduction
2. Moore's law
3. Brief introduction to MOSFET transistors
4. Evolution of transistor technology
5. Race of the IC vendors
6. References

## Slide 3
1. Introduction
Notes: 3

## Slide 4: 1. Introduction (1)
Example: 22 nm Ivy Bridge chips on a 300 mm wafer [1]
Manufacturing of processor chips
Processor chips are produced on wafers, as seen in the example below.
1. Introduction

## Slide 5: 1. Introduction (2)
2"
4"
6"
8"
Early evolution of wafer sizes [2]

## Slide 6: 1. Introduction (3)
Subsequent evolution of wafer sizes [3]

## Slide 7: 1. Introduction (4)
Introduction dates of larger wafer sizes [4]

## Slide 8: 1. Introduction (5)
Historic distribution of wafer sizes actually produced [4]

## Slide 9: 1. Introduction (6)
Visual checking of chips [5]

## Slide 10: 1. Introduction (7)
The IC production process
IC production needs 200 - 300 process steps, based on a number of masks, and includes
steps such as diffusion, etching, checkings etc..
The whole production process lasts about two to three months.
IC production facilities are called foundries or fabs.

## Slide 11: 1. Introduction (8)
Internal view of a part of a foundry [6] -1

## Slide 12: 1. Introduction (9)
Internal view of a part of a foundry [7] -2

## Slide 13: 1. Introduction (10)
Bird's eye view of a foundry
Figure: Bird's eye view of Globalfoundries Fab 8 in New York (2012) producing 32 nm chips [8]

## Slide 14: 1. Introduction (11)
The cost for establishing a foundry
About 3 - 10 billion USD, increasing for smaller feature sizes.

## Slide 15: 1. Introduction (12)
Kw/m: Kilowafer per month in 200 mm equivalents
Production capacity of major vendors with foundries [9]
Fabs which overtake orders for IC fabrication

## Slide 16: 1. Introduction (13)
Sales revenues of the top 20 chip vendors (million USD) [10]
Pure-play foundry: A foundry without any semiconductor design capability.

## Slide 17: 1. Introduction (14)
Number of foundries owned by major firms
Major firms have a number of foundries for each current feature size (e.g. for 22 nm, 14/16 nm)
and also they continuoualy invest to build next generation fabs (e.g. recently 10 nm fabs).

## Slide 18: 1. Introduction (15)
Example: Intel’s 22 nm foundires [1]

## Slide 19: 1. Introduction (16)
Characterizing process technology
Traditionally, IC process technologies are characterized by the minimum feature size.
Interpretation of the minimum feature size for MOS transistors:
It is the minimum length of the MOS transistor channel between the drain and the source.
Accordingly, the minimum feature size was interpreted traditionally as the gate length,
as indicated below:

## Slide 20: 1. Introduction (17)
Recent interpretation of the minimum feature size
It identifies the process technology of a given IC foundry (e.g. to be 22 nm or 14 nm node).
Then, process parameters cannot be simple derived from the feature size as before,
instead, select parameters relating to the same technology node can differ significantly, e.g.
by 20 %, from each other for the same process implemented by different vendors, as seen
in the Table below.
Table: MOS transistor parameters of different foundries belonging to 14 to 22 nm nodes [5]
Recently, the minimum feature size is interpreted as the technology node.

## Slide 21: 1. Introduction (18)
For process technologies (rougly below 300 nm) the gate length became shorter than the
minimum feature size (node), as shown below for Intel's MOS processes.
Figure: Gate length in Intel's subsequent MOS technologies [11]
As an example, in Intel's 65 nm technology the gate length amounts only to 35 nm.
Shortening the minimum feature size in the course of the evolution of IC technology
Gate length
Minimum feature size

## Slide 22: 1. Introduction (19)
Illustrating a feature size of 10 nm [12]

## Slide 23: 1. Introduction (20)
AMD at CES 2016 Polaris
Historical evolution of AMD's GPU chip technology [13]

## Slide 24
2. Moore's law
Notes: 24

## Slide 25: 2. Moore’s law (1)
First planar transistors (~1959) and first integrated circuits (~1961) [14]
2. Moore's law

## Slide 26: 2. Moore’s law (2)
Original publication of Moore's law in 1965, stating that transistor counts double roughly
every year [15]

## Slide 27: 2. Moore’s law (3)
Moore’s original projection for increasing the number of components per IC [14]
Moore’s law

## Slide 28: 2. Moore’s law (4)
First commercially usable memory or microprocessor chips (1 Kb DRAMs, 4-bit microprocessors)
needed n×103 transistors, as seen in the Figure below.
Implication of Moore's law to the emergence of 1K DRAMs and microprocessors -1

## Slide 29: 2. Moore’s law (5)
Intel's first 1 Kbit dynamic DRAM chip, the 1103 (Oct. 1970)
1 Kx1-bit structure, pMOS technology, 3T (three-transistors per bit) design,
two power supplies (+16 V/+19 V), non-multiplexed addressing, 18-pin package.
Figure: Intel’s 1103 [17]
Main features:
Figure: Die photo of Intel’s 1103 [18]

## Slide 30: 2. Moore’s law (6)
2300
transistors
Introduced:
11/1971
Intel's first microprocessor, the 4004 [16]

## Slide 31: 2. Moore’s law (7)
Figure: The rise of IC complexity (following Moore’s low) [14]
Due to Moore’s (oroginal) low, the integration of 210 transistors on a chip needs ~ 10 years.
Implication of Moore's law to the emergence of 1K DRAMs and microprocessors -3
1970/1971 became the birth years of DRAMs and microprocessors.
The implementation of first DRAMs and microprocessors needed a few thousand transistors.

## Slide 32: 2. Moore’s law (8)
Moore’s revised law from 1975 [14]
~2x/1 year
~2x/2 years

## Slide 33: 2. Moore’s law (9)
The actual rise of IC complexity in DRAMs and microprocessors [14]
~2x/1 year
~2x/2 years

## Slide 34: 2. Moore’s law (10)
Scaling: ~ 0.7/2 years
The underlying reason for Moore's law
In fact, Moore's law results from the cadence of the evolution of IC manufacturing technology.
The Figure below shows as an example the evolution of Intel's IC manufacturing technology
between 1995 and 2006.
Figure: Evolution of Intel's IC manufacturing technology between 1995 and 2006 -1 [Intro to multicores 1]

## Slide 35: 2. Moore’s law (11)
Derivation of Moore's law from the scaling of IC manufacturing technology
Moore’s law
In every two years the same number of transistors can be implemented on ~ ½ Si die area
Assumed scaling of IC manufacturing: ~ 0.7x/2 years
In every two years ~ 2x more transistors can be implemented on the same die area
or

## Slide 36: 2. Moore’s law (12)
The last two technology transitions have signaled that our cadence today is closer to 2.5 years than two“ [37].
On Intel’s Q2 2015 earnings conference call, on July 16 2015, Krzanich: in the second half of 2017, we expect
to launch our first 10-nanometer product, code named Cannonlake.
Lengthening the cadence of Intel’s technology transitions [36]
2000
2002
2004
2006
2008
2010
2012
2014
2016
2018
200
180
160
140
120
100
80
60
40
0
20
180 nm
130 nm
90 nm
65 nm
45 nm
32 nm
22 nm
14 nm
10 nm
Pentium 4
Northwood
Pentium 4
Prescott
Pentium 4
Cedar Mill
Penryn
Westmere
Ivy Bridge
Broadwell
Pentium 4
Willamette
Cannonlake
01/02
02/04
11/07
01/10
04/12
09/14
11/00
2H/17
01/06
nm

## Slide 37: 2. Moore’s law (13)
High-End Desktops
Servers
High-End Desktops
Desktops
Laptops
Smartphones
Tablets
Core counts in computing devices
Mobiles
Traditional computers
Typical no.
of CPU cores
Up to 28
Up to 10
2 to 4
2 to 4
4 to 8
4 to 8

## Slide 38: 2. Moore’s law (14)
Core count
2006
2008
2010
2012
2014
2016
Year
7000
(90 nm)
7300
(65 nm)
7400
(45 nm)
Nehalem-EX
(45 nm)
Westmere-EX
(32 nm)
Ivy-Bridge-EX
(22 nm)
Broadwell-EX
(14 nm)
*
*
*
*
*
2
4
8
16
32
24
10
6
15
*
*
~2x/4 years
~2x/2 years
The rate of rising core counts in Intel's servers

## Slide 39: 2. Moore’s law (15)
Core count
2006
2008
2010
2012
2014
2016
Year
K8/800
Egypt
(90 nm)
K10/8300
Barcelona
(65 nm)
K10.5/8400
Istambul
(45 nm)
Bulldozer 6200
2xOrochi die
(32 nm)
Piledriver 6300
2xWarsaw die
(32 nm)
*
*
*
*
*
2
4
8
16
32
24
10
6
15
< 2x/4 years
~2x/2 years
12
Piledriver 6300
2xAbu Dhabi die
(32 nm)
K10.5 6100
2xIstambul die
(45 nm)
?
The rate of rising core counts in AMD's servers

## Slide 40: 2. Moore’s law (16)
2006
2008
2010
2012
2014
2016
Year
2000
2002
2004
Transfer rate
(MT/s)
200
400
800
1600
2400
1000
600
*
*
*
*
DDR2
533
DDR2
666
DDR2 800
DDR3
1600
DDR3
1066
*
*
DDR3
1333
*
DDR4/2133
DDR3/1866
*
*
*
DDR
333
~ 2*/8 years
t0
x
x
x
x
x
*
DDR
400
DDR2
666
DDR3
1600
DDR3
1866
DDR
400
DDR3
1066
DT
MP
DDR
266
1200
2000
  ~ 2*/4 years
The rate of rising memory transfer rates in Intel's DT and MP platforms

## Slide 41: 2. Moore’s law (17)
Aftermath of the fact that memory speeds rise slower than core counts
In servers core counts rise as fast as technology allows but memory speeds increase
at a slower rate, as seen in the Figures before.
On the other hand to avoid memory bandwidth bottlenecks multicores need proportionally
more bandwidth than single core processors, i.e. an 8-core processor needs 8-times more
bandwidth than a single core processor.
It can be shown that in multicore servers while in subsequent generations both core counts
and memory speeds rise, albeit at different rates, the number of memory channels needed
for providing the same per core memory bandwidth as a baseline design is proportional
with the square root of the core count.
It means that doubling core counts in a baseline design requires approximately √2 times more
memory channels related to the baseline design.
As a consequence, designing the memory subsystem of multicore servers with ever raising
core counts is a sensitive and intricate issue, as discussed in a related Chapter.

## Slide 42
3. Brief introduction to MOSFET transistors
It will not be discussed.
Notes: 42

## Slide 43: 3. Brief introduction to MOSFET transistors (1)
3. Brief introduction to MOSFET transistors
MOSFET: Metal-OXid-Semiconductor Field-Effect Transistor
MOSFET is often abreviated as MOS.
pMOS transistors
MOSFET transitors
nMOS transistors
For simplicity, we consider only enhancement mode MOS transistors, as these devices are
the most common building elements of microprocessors.
Enhancement mode MOS transistors are off when the gate-source voltage is zero and will be
turned on for appropriate positive values of the gate-source input voltage.

## Slide 44: 3. Brief introduction to MOSFET transistors (2)
Internal structure of the nMOS (nMOSFET) transistor [19]
The Source and the Drain are implemented as two highly (n+) doped diffusion regions.
Dpoing (e.g. by arsenid) aims at providing additional free electrons.
The area in-between forms a channel with controllable conductivity.
The Gate is built from a conductor, typically polysilicon, and is insulated from the Source-
Channel-drain structure by a layer of silicon dioxide (SiO2).
The voltage between the gate and the substrate induces an electric field which controls the
flow of electrons in the channel.
This gives rise to the name: Field-Effect Transistor (FET).

## Slide 45: 3. Brief introduction to MOSFET transistors (3)
Operation of the nMOS transistor [19] -1
Switched off region of the operation
The nMOS transistor has three operational regions.
If the Gate-Source voltage (VGS) is less than the Thrashold voltage (VT) (i.e. if VGS < VT)
the transistor is switched off, no Drain current is flowing, as the Figure on the left shows.
The transistor is also in the switched off state when VDS = 0, as indicated in the Figure
on the right.
Figure: ID vs. VGS and ID vs. VDS characteristics of the nMOS transistor [19]

## Slide 46: 3. Brief introduction to MOSFET transistors (4)
b) Linear region of the operation
If VGS > VT and 0 < VDS < VSAT, the transistor operates in the linear state,
as the Figure on the right shows.
Figure: ID vs. VGS and ID vs. VDS characteristics of the nMOS transistor [19]
Operation of the nMOS transistor [19] -2
VSAT

## Slide 47: 3. Brief introduction to MOSFET transistors (5)
Using the linear region of operation of an nMOSFET transisitor to built an amplifier [20]

## Slide 48: 3. Brief introduction to MOSFET transistors (6)
c) Saturation region of the operation
If VGS > VT and VDS > VSAT (VDS) , the transistor operates in the saturation state,
as the Figure on the right shows.
Figure: ID vs. VGS and ID vs. VDS characteristics of the nMOS transistor [19]
Operation of the nMOS transistor [19] -3
VSAT
, VGS > VT
, VGS > VT

## Slide 49: 3. Brief introduction to MOSFET transistors (7)
In the saturation region the nMOS transistor operates as a controlled switch, as indicated below.
Using an nMOS transistor as a switch
VSS
VGS = VDD
VGS = 0
On
Off
VDS
VDS = VDD
VDS = VDD
VGS

## Slide 50: 3. Brief introduction to MOSFET transistors (8)
Remark: Physical background of the operation of the enhancement mode nMOS transistor [19] -1
Switched off state
a1) Switched off stated due to VGS < VT (VDS is irrelevant and can be 0)
Figure: Formation of a depletion region in an enhancement-mode nMOS FET [19].
The electric field induced by the gate voltage points down from the gate through the
channel.
This fields repels the majority carriers (that is positive holes) of the p-type substrate,
from the channel hence forming a region depleted of carriers as shown in the Figure
above.
As a result, due to the lack of free carriers, no current will flow between the source and
the drain in this case, that is, ID = 0.
The threshold voltage VT depends on the actual fabrication technology and usually is
about 0.5V.

## Slide 51: 3. Brief introduction to MOSFET transistors (9)
Figure: Formation of the
conducting channel (inversion layer) in an enhancement mode nMOS [19].
When the gate voltage VGS increases above the threshold voltage VT, then the electric field
repels more holes from the channel area leaving an excess of electrons.
The field also pulls out electrons from the source and drain areas which have excess of
electrons since they are n+ regions.
As a result, in the channel area an inversion layer is formed in which there is an excess of
negative carriers, that is, electrons.
In other words a conducting channel has been formed between the source and drain.
But as the drain-source voltage is assumed to be 0, (VDS = 0) no drain corrent ID flows
in the channel (ID = 0).
Remark: Physical background of the operation of the enhancement mode nMOS transistor [19] -2
a2) Switched off stated due to VGS > VT and VDS = 0

## Slide 52: 3. Brief introduction to MOSFET transistors (10)
b) Linear state
If VGS > VT and 0 < VDS < VSAT
Figure: an nMOS
transisitor operating
in the linear region.
In this case, there are free electrons in the conducting channel, and when the drain-source
voltage increases above zero, VDS > 0, the negative carriers (electrons) will flow from the
source to the drain, resulting in a source-drain current, i.e. ID starts to flow.
When the VDS voltage is relatively small, the transistor operates in the so-called linear
region.
In this region of operation the drain current ID is a quadratic function of the source-drain
voltage, VDS.
Remark: Physical background of the operation of the enhancement mode nMOS transistor [19] -3

## Slide 53: 3. Brief introduction to MOSFET transistors (11)
c) Saturation state
If VGS > VT and VDS > VSAT (VDS) , the transistor operates in the saturation region.
When the source-drain voltage, VDS, reaches a certain value, Vsat, the channel depth at the
drain end is reduced to zero.
This is called the pinch-off point (leszűkülési pont).
In other words, at the pinch-off point, VDS = Vsat.
From now on, a further increase of the source-drain voltage does not result in an increase
of the source-drain current and the transistor operates in the saturation mode.
Figure: the nMOS
transistor operating
in the saturation region.
Remark: Physical background of the operation of the enhancement mode nMOS transistor [19] -4

## Slide 54: 3. Brief introduction to MOSFET transistors (12)
Internal structure of the pMOS transistor [19]
As seen in the Figure, in p-type FET (pMOS) p- and n-types are exchanged.

## Slide 55: 3. Brief introduction to MOSFET transistors (13)
CMOS (Complementary-Metal-Oxid semiconductor) inverter
Figure: Schematics of a CMOS inverter [21]
A CMOS inverter consists of a pMOS and an nMOS transistor connected in series,
as indicated in the Figure below.

## Slide 56: 3. Brief introduction to MOSFET transistors (14)
Simplified principle of operation: From both switches one is on and the other one is off.
For low input voltages the pMOS transistor is on, the nMOs transistor is off and accordingly
the output is high.
By contrast, for high input voltages the pMOS transistor is off, the nMOs transistor is on
and accordingly the output is low.
Simplified view of the operation of the inverter
In a simplified view the inverter operates as two switches connected in series, as seen below.
Schematics of an inverter
Simplified view of its operation
Vout
Vin
+Vdd
VSS (GND)
Drain
Drain
Source
pMOS
switch
nMOS
switch
If Vin is low
pMOS switch is on,
nMOS switch is off
Vout = +Vdd
If Vin is high
pMOS switch is off,
nMOS switch is on
Vout = Vss (GND)
Vin
+Vdd
Drain
Drain
Gate
Gate
Source
Source
pMOS
nMOS
Vout
VSS (GND)
Gate
Gate
Source

## Slide 57: 3. Brief introduction to MOSFET transistors (15)
Figure: a) Schematics of the inverter, b) Transfer characterisctics of the inverter (Vout vs. Vin),
c) Inverter current vs. input voltage (Vin) [22]
A more accurate description of the operation of the CMOS inverter -1
The operation of a CMOS inverter can be described more accurately by its transfer and current
characteristics, see the Figure below.

## Slide 58: 3. Brief introduction to MOSFET transistors (16)
A more accurate description of the operation of the CMOS inverter -2
Note
As figure c) indicates, the CMOS circuit draws current only when it is switched from
one logic state to another.
Consequently, CMOS circuits consumes significantly less power than TTL or nMOS circuits,
which draw current in the on state.
This is the main reason why microprocessors are typically built up of CMOS logic.
Another benefit of the CMOS circuits is their high noise immunity resulting from the
saturation mode operation.

## Slide 59: 3. Brief introduction to MOSFET transistors (17)
Implementation of a CMOS inverter on a Si die [21]

## Slide 60
4. Evolution of transistor technology
4.1 Overview
4.2 The scaling law of MOSFET technology
4.3 Strained Si technology
4.4 The HKMG transistor
4.5 FinFET transisitors
Notes: 60

## Slide 61
4.1 Overview of the evolution of transistor technology
Notes: 61

## Slide 62: 4.1 Overview of the evolution of transistor technology (1)
Historical data on scaling down IC tecnology [23]
4.1 Overview of the evolution of transistor technology
Remark
Until recently typically Intel lead the way for scaling down feature sizes.
10 µm | 1971
6 µm | 1974
3 µm | 1977
1.5 µm | 1982
1 µm | 1985
800 nm | 1989
600 nm | 1994
350 nm | 1995
250 nm | 1997
180 nm | 1999
130 nm | 2001
90 nm | 2004
65 nm | 2006
45 nm | 2008
32 nm | 2010
22 nm | 2012
14 nm | 2014
10 nm | 2017
7 nm | 2019

## Slide 63: 4.1 Overview of the evolution of transistor technology (2)
Overview of scaling down feature sizes in Intel’s basic microarchitectures (Based on [24])
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.
1/2008
1/2010
Clarkdale
4/2012
9/2014

## Slide 64: 4.1 Overview of the evolution of transistor technology (3)
Main contributions for the evolution of transistor technology
Main contributions for the evolution of transistor technology
FinFET
transistors
The scaling law of
MOSFET technology
HKMG
transistors
Strained
silicon technology
45/32 nm
22 nm and below
90/65 nm
Used by Intel at
130 nm and before
Section 4.2
Section 4.3
Section 4.4
Section 4.5
MOSFET: Metal Oxid Fied Effect Transistor: MOS Térvezérlésű Tranzisztor

## Slide 65: 4.1 Overview of the evolution of transistor technology (4)
Decreasing the core voltage (and dissipation) in Samsung's subsequent IC processes [25]

## Slide 66
4.2 The scaling law of MOSFET technology
Notes: 66

## Slide 67: 4.2 The scaling law of MOSFET technology (1)
4.2 The scaling law of MOSFET technology
The early evolution of transistor manufacturing technology was marked by scaling down
its structure.
The principle of scaling were laid down by a paper of Dennard in 1974 [26] based on research
work done by IBM.
Figure. Illustration of scaling down a transistor structure (commercially available at the
time of the publication) by a linear factor of k=5 [26]
Dennard's paper presumes a linear scaling of the transistor dimensions, as shown below.

## Slide 68: 4.2 The scaling law of MOSFET technology (2)
Scaling down MOSFET transistor structures
The cited publication states how circuit parameters have to be be scaled down,
(see the Table below).
Table: Scaling of transistor and circuit parameters [26]
As the Table shows when scaling down transistor dimensions by a factor of k, relevant
transistor parameters, such as transistor dimensions, the supply voltage, currents need
also be scaled down by the same factor k.
Scaling down of transistor dimensions by a factor of k ideally reduces delay time by a factor
of k and the power dissipation of the circuit by a factor of k2.
Here we note that albeit the power dissipation of a single transistor is scaled down by k2,
there are now k2 times as many transistors on the same area as before, so a die of the
same dimensions as before consumes the same power as before. in other words
the power density remains constant.

## Slide 69: 4.2 The scaling law of MOSFET technology (3)
Intel's 65 nm transistor
structure (2005)
Transistor structure
in the middle of the 1970's
Contrasting scalied down transistor structures from the middle of 1970's to about 2005
[11]

## Slide 70: 4.2 The scaling law of MOSFET technology (4)
Limits of Dennard's scaling law
Dennard's paper neglects two points that became successively more critical, as follows [11].
At the time of the publication leakage currents could be ignored, as they were on the
order of 10-10, but subsequently till introducing the 65 nm technology they have
increased many orders of magnitude.
Another key point of Dennard's paper was the assumption that gate oxid thickness can be
scaled down further on for a long time.
Here we note that in 65 nm technology the SiO2 dielectric is only 1.2 nm thick.
At this thickness the dielectric is only about 4 to 5 atomic layers thick and does not allow
a further scaling.
The diameter of a Si atom is ~ 110x10-12 m = 0.1x10-9 m = 0.1 nm
Remark
Due to these limitations - more or less at achieving the 65 nm technology, Dennard's
scaling law could not be followed further on for reducing transistor structures but
it became necessary to introduce a number of innovations, as discussed next.

## Slide 71
4.3 Strained Si technology
Notes: 71

## Slide 72: 4.3 Strained Si technology (1)
4.3 Strained Si technology
Principle
By using appropriate IC technologies the Si lattice becomes strained, i.e. the distance betwen
the Si atoms becomes wider, as indicated in the Figure below.
Figure: Principle of the strained Si technology [27]

## Slide 73: 4.3 Strained Si technology (2)
Benefits and drawbacks of the strained Si technology [27]
It increases electron and hole mobility.
Greater mobility results in 10-20 % increase drive currents that raises performance.
The strained Si process needs a few additional process steps that increase the total process cost
by less than 2 %.
Benefits
Drawback

## Slide 74
4.4 The HKMG transistor
Notes: 74

## Slide 75: 4.4 The HKMG transistor (1)
Figure: Intel’s Tick-Tock development model (Based on [24])
4.4 The HKMG transistor
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.
HKMG means High-k Metal Gate.
HKMG transistors has been introduced by Intel along with the Penryn family of processors in 2007.

## Slide 76: 4.4 The HKMG transistor (2)
Example iplementation
of the gate oxid layer at 90 nm
Layout of an nMOS transistor
Limitation of MOSFET scaling in respect to the gate oxid (insulator) layer [28]
When transistor structures have been scaled down to about 90 or 65 nm the width of the SiO2
layer became as short as about 1 nm.
However, the distance between SiO2 molecules is about 0.3 nm so for example a 1.2 nm SiO2
layer is only about 4 SiO2 molecules wide [29].
As a consequence, while transistor structures were scaled down to the low feature sizes of
90 or 65 nm the leakage current rose drastically, as the next figure shows.

## Slide 77: 4.4 The HKMG transistor (3)
Figure 3.1.1: Dynamic and static power dissipation trends in chips [30]
Sub-threshold =
Source-Drain
The need to introduce new transistor design [30]

## Slide 78: 4.4 The HKMG transistor (4)
Where
A is the capacitor area
κ is the relative dielectric constant of the material (3.9 for SiO2 and > 10 for a high k dielectric)
ε0 is the permittivity of free space
t is the thickness of the capacitor oxide insulator
The gate oxide layer in a MOSFET can be modeled as a parallel plate capacitor.
The capacitance C of this parallel plate capacitor is given by
1.2 nm SiO2
Principle of the HKMG transistor [28]

## Slide 79: 4.4 The HKMG transistor (5)
The thin SiO2 insulator layer can be replaced by a wider high-k dielectric that provides the same
or higher capacitance, as shown below.
The wider high-k insulator layer results in considerable less leakage current, as the Figure
indicates.
Principle of reducing the leakage current [28]

## Slide 80: 4.4 The HKMG transistor (6)
Structure of the HKMG (High-k + Metal Gate) transistor [31]

## Slide 81: 4.4 The HKMG transistor (7)
Benefits of HKMG transistors [31]

## Slide 82
4.5 FinFET transistors
4.5.1 Introduction to the FinFET transistors
4.5.2 Intel's 22 nm FinFET transistor
4.5.3 Intel's 14 nm FinFET transistor
Notes: 82

## Slide 83
4.5.1 Introduction to the FinFET transistors
Notes: 83

## Slide 84: 4.5.1 Introduction to the FinFET transistors (1)
Intel's FinFET generations
Intel's 22 nm FinFET transistor
Intel's 14 nm FinFET transistor
First generation FinFET
Second generation FinFET
Ivy Bridge line (4/2012)
The FinFET transistor is termed also as Tri-gate or 3D transistor.
The term FinFET (Fin Field Effect Transistor) was coined in 1999 by researchers at the
University of California, Berkley, nevertheless, first commercial implementations appiered
only more than 10 years later in 2012 by Intel under the designation Tri-gate transistor.
There is no consensus about how to designate MOS tranasistor structures using fins,
a few firms like IBM, AMD or the foundries TSMC or GlobalFoundries make use of the term
FinFET whereas Intel dubs such transistor structures as Tri-gate transistors.
Appeared along with
Broadwell line (6/2015)
4.5.1 Introduction to the FinFET transisitors
Until now Intel developed two generations of FinFET transistors.

## Slide 85
4.5.2 Intel's 22 nm FinFET transistor
Notes: 85

## Slide 86: 4.5.2 Intel’s 22 nm FinFET transistor (1)
Introduced along with the Ivy Bridge family of processors in 2012.
Figure: Intel’s Tick-Tock development model (Based on [24])
4.5.2 Intel's 22 nm FinFET transistor -1
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 87: 4.5.2 Intel’s 22 nm FinFET transistor (2)
The traditional planar transistor [1]

## Slide 88: 4.5.2 Intel’s 22 nm FinFET transistor (3)
The 22 nm FinFET transistor -2 [1]
The designation “tri-gate” originates from the fact that now the gate has three sides.
fin

## Slide 89: 4.5.2 Intel’s 22 nm FinFET transistor (4)
The 22 nm FinFET transistor -3 [1]

## Slide 90: 4.5.2 Intel’s 22 nm FinFET transistor (5)
Contrasting 2D planar and 3D FinFET transistor structures [38]

## Slide 91: 4.5.2 Intel’s 22 nm FinFET transistor (6)
Switching characteristics of the traditional planar and FinFET transistors [1]

## Slide 92: 4.5.2 Intel’s 22 nm FinFET transistor (7)
Gate delay of the traditional planar and FinFET transistors [1]
Gate delay: time difference between output signal and input signal of a gate (n x ps)

## Slide 93: 4.5.2 Intel’s 22 nm FinFET transistor (8)
Intel’s 22 nm FinFET manufacturing fabs [1]

## Slide 94
4.5.3 Intel's 14 nm FinFET transistor
Notes: 94

## Slide 95: 4.5.3 Intel’s 14 nm FinFET transistor (1)
Figure: Intel’s Tick-Tock development model (Based on [24])
4.5.3 Intel's 14 nm FinFET transistor-1
Introduced along with the Broadwell family of processors in 2014
Core 2
New
Microarch.
65 nm
Penryn
New
Process
45 nm
Nehalem
New
Microarch.
45 nm
West-
mere
New
Process
32 nm
Sandy Bridge
New
Microarch.
32 nm
Ivy Bridge
New
Process
22 nm
Haswell
New
Microarchi.
22 nm
TOCK
TICK
TOCK
TICK
TOCK
TICK
TOCK
1. gen.
2. gen.
3. gen.
4. gen.
5. gen.
Broad-
well
New
Process
14 nm
TICK
Skylake
New
Microarchi.
14 nm
TOCK
6. gen.

## Slide 96: 4.5.3 Intel’s 14 nm FinFET transistor (2)
14 nm 2 generation FinFET transistors with fin improvement [12]

## Slide 97: 4.5.3 Intel’s 14 nm FinFET transistor (3)
14 nm Broadwell SOC yield trend [12]

## Slide 98: 4.5.3 Intel’s 14 nm FinFET transistor (4)
Benefits of reducing the feature size [12]
New technology generations provide improved performance and/or reduced power,
but the key benefit is improved performance/Watt.

## Slide 99: 4.5.3 Intel’s 14 nm FinFET transistor (5)
Leakage power vs clock speed for smaller feature sizes [12]
fc > Vc for const. nm
Vc > Il > Ds

## Slide 100: 4.5.3 Intel’s 14 nm FinFET transistor (6)
Leakage power vs. clock speed for smaller feature sizes in different product sectors [12]

## Slide 101
5. Race of the IC vendors
Notes: 101

## Slide 102: 5. Race of the IC vendors (1)
5. Race of the IC-vendors [32]
Main steps in the evolution of Intel's transistor technology [32]

## Slide 103: 5. Race of the IC vendors (2)
Evolution of Intel's transistor technology from 130 nm to 32 nm [33]

## Slide 104: 5. Race of the IC vendors (3)
Intel's lead in introducing new transistor technologies [15]

## Slide 105: 5. Race of the IC vendors (4)
Slowing down the cadence of the evolution of Intel’s process technologies
in light of Intel's technology roadmap published in 5/2011 [1]
2015
HKMG
FinFET
1. gen.
FinFET
2. gen.
New transistor
structures
Penryn
Ivy Bridge
Broadwell
Related
proc. family
2017?

## Slide 106: 5. Race of the IC vendors (5)
Intel’s relative yield trends of their 14 nm technology vs. their 22 nm technology [12]

## Slide 107: 5. Race of the IC vendors (6)
Intel’s lead in IC technology up to the 22/20 nm node, according to [12]
Source: Intel 08/2014
Others:
TSMC (Taiwan)
GlobalFoundries (Abu Dhabi)
( AMD Microelectronic 2009)
( IBM Microelectronic 2015)
Samsung Semiconductor
(South Korea)
Intel
Logic area scaling

## Slide 108: 5. Race of the IC vendors (7)
 | Intel | TMSC | Global Foundries (Acquired AMD/IBM) | Samsung
45nm | HKMG: 11/2007 (Penryn) | - | 1/2009 (Phenom II) | End of 2007
40nm | - | 4/2009 (RV740) | - | 
32nm | 1/2010 (Westmere Clarkdale) | - | HKMG: 6/2011 (Llano) | HKMG: 6/2010
28nm | - | HKMG: 1/2012 (Tahiti) | 1/2014 (Kaveri) | 9/2013 (Apple A7)
22nm | FinFET 4/2012 (Ivy Bridge) | - | - | 
20nm | - | Roadmap: Begin of 2013 SoC-products: 1/2014 | Left out in favour of 14 nm technology | 
16nm | - | Roadmap: 11/2013 FinFET FF+: 7/2015 | - | 
14nm | Roadmap: 2013 Advanced FinFET CPU-products: 9/2014 (Broadwell) | - | Roadmap: End of 2014 Development cancelled Technology licenced from Samsung (4/2014) | FinFET LPE: 2/2015 FinFET PPE: 1/2016
10nm | Roadmap: 2015 Products expected: 2H/2017 (Cannonlake) | Roadmap: 2016 Products expected: Early 2017 | Roadmap: End of 2015 Products expected: 2017 | Late 2016
7nm | Roadmap: 2017 Products expected: 2018 or 2019 | 2018 | ? | ?
HKMG | With 45 nm (2007) | With 28 nm (2012) | With 32 nm (2011) | With 32 nm (2010)
3D-Transistors | With 22nm (2012) | With 16nm (2015) | With 14 nm (2015) | With 14 nm (2015)
Evolution of IC technology by leading foundries (Partly based on [34])

## Slide 109: 5. Race of the IC vendors (8)
Cooperation of Samsung and GlobalFoundries in 14 nm FinFET production [35]

## Slide 110
Samsung's position - Despite the Korean war 1950 -1953 [39], [40]
Headquarter: Seoul

## Slide 111
6. References
Notes: 111

## Slide 112
6. References (1)
[2]: Wikipedia, Wafer (electronics),
https://en.wikipedia.org/wiki/Wafer_(electronics)
[3]: The Evolution of AMHS, Daifuku, Jan. 2012,
http://www.daifuku.com/solution/technology/semiconductor/
[1]: Bohr M., Mistry K.: Intel’s Revolutionary 22 nm transistor technology, May 2011,
http://download.intel.com/newsroom/kits/22nm/pdfs/22nm-Details_Presentation.pdf
[4]: Hruska J., Atom Everywhere: Intel breaks ground on first 450mm fab, Extreme Tech,
Aug. 7 2013, http://www.extremetech.com/extreme/163372-atom-everywhere-intel-
breaks-ground-on-first-450mm-fab
[5]: Hruska J., TSMC will begin 10nm production this year, claims 5nm by 2020, Extreme Tech,
Jan. 20 2016, http://www.extremetech.com/computing/221532-tsmc-will-begin-10nm-
production-this-year-claims-5nm-by-2020
[6]: Shilov A., GlobalFoundries to produce 14nm chips in the first half of 2015, KitGuru,
Dec. 18 2014, http://www.kitguru.net/components/graphic-cards/anton-shilov/
globalfoundries-to-produce-14nm-chips-in-the-first-half-of-2015/
[7]: Farrell N., TSMC promises 7nm chips in 2017, Fudzilla, April 22 2015,
http://www.fudzilla.com/news/processors/37587-tsmc-promises-7nm-chips-in-2017
[8]: Shilov A., Globalfoundries' Fab 8 Begins to Produce First Commercial Chips for Customers,
Xbit Labs, Jan. 11 2012, http://www.xbitlabs.com/news/other/display/20120111101201_
Globalfoundries_Fab_8_Begins_to_Produce_First_Commercial_Chips_for_Customers.html

## Slide 113
6. References (2)
[10]: Clarke P., Sales declines dominate 1Q16 chip vendor ranking, EE Times, May 23 2016,
http://www.electronics-eetimes.com/news/sales-declines-dominate-1q16-chip-vendor-ranking-0
[11]: Bohr M., A 30 Year Retrospective on Dennard's MOSFET Scaling Paper, IEEE-SSCS, 2007,
http://www.eng.auburn.edu/~agrawvd/COURSE/READING/LOWP/Boh07.pdf
[9]: Top Semiconductor Foundries Capacity 2015-2016 (Infographic), Anysilicon, Jan. 21 2016,
http://anysilicon.com/top-semiconductor-foundries-capacity-2015-2016-infographic/
[12]: Bohr M., 14 nm Technology Announcement, Aug. 11 2014, Intel,
http://download.intel.com/newsroom/kits/14nm/pdfs/Intel_14nm_New_uArch.pdf
[13]: Mujtaba H., NVIDIA Pascal GPU Analysis – An In-Depth Look at NVIDIA’s Next-Gen Graphics
Cards Powering GeForce, Tesla and Quadro, WCCF Tech, Jan. 13 2016,
http://wccftech.com/nvidia-pascal-gpu-analysis/
[14]: Moore G. E., No Exponential is Forever... ISSCC 2003,
ftp://download.intel.com/research/silicon/Gordon_Moore_ISSCC_021003.pdf
[15]: Holt W., Advancing Moore's Law: Benefits Across the Portfolio, Investor Meeting, Nov. 21 2013,
http://www.semiwiki.com/forum/files/Intel%20Manufacturing%20Slides%202013.pdf
[16]: Myslewski R., Happy 40th birthday, Intel 4004! The first of the bricks that built the IT world,
The Register, Nov. 15 2011, http://www.theregister.co.uk/2011/11/15/the_first_forty_
years_of_intel_microprocessors/?page=2
[17]: 2116 Family, 16384 x 1 Bit Dynamic RAM, Data Catalog, Intel, 1977

## Slide 114
6. References (3)
[19]: Paplinski A.P., CSE3142 Integrated Circuit Design, Monash University, 2006,
http://www.csse.monash.edu.au/courseware/cse3142/2006/Lnts/C02.pdf
[20]: MOSFET Amplifier, Electronics Tutorials,
http://www.electronics-tutorials.ws/amplifier/mosfet-amplifier.html
[18]: Intel Museum, Historical Documents,
http://download.intel.com/museum/research/arc_collect/history_docs/pix/1103.jpg
[21]: CMOS LOGIC Family, Emaze, https://www.emaze.com/@AIRQLQR/CMOS-LOGIC-FAMILY
[22]: NMOS Inverter vs CMOS Inverter -- transfer characteristics, Edaboard, July 19 2014,
http://www.edaboard.com/thread319744.html
[23]: Wikipedia, 32 nanometer, https://en.wikipedia.org/wiki/32_nanometer
[24]: Singhal R., “Next Generation Intel Microarchitecture (Nehalem) Family: Architecture Insight
and Power Management, IDF Taipeh, Oct. 2008, http://intel.wingateweb.com/taiwan08/
published/sessions/TPTS001/FA08%20IDFTaipei_TPTS001_100.pdf
[25]: Woo NS., Samsung System LSI Business, 2013,
http://www.slideshare.net/fullscreen/bassilis/samsung-analyst-day-2013-slsi-namsung-
woo-samsung-system-lsi-business/15
[26]: Dennard R.H., Gaensslen F.H., et al., Design of Ion-Implanted MOSFET’S with Very Small
Physical Dimensions, IEEE Journal of Solid State Circuits, Oct. 1974,
http://www.eng.auburn.edu/~agrawvd/COURSE/READING/LOWP/Design%20of%20ion-
implanted%20MOSFETs%20with%20very%20small%20physical%20dimensions.pdf

## Slide 115
6. References (4)
[28]: Wikipedia, High-κ dielectric,
https://en.wikipedia.org/wiki/High-%CE%BA_dielectric
[29]: Misra D., Iwai H., Wong H., High-k Gate Dielectrics, The Electrochemical Society, 2005,
https://www.electrochem.org/dl/interface/sum/sum05/IF08-05_Pg30-34.pdf
[27]: Walden J., 90 nm and Beyond: Moore's Law and More, 2002,
http://www.eet.bme.hu/~mizsei/Nanoelektronika/vlsifuture03.pdf
[30]: Kim N. S. et al., „Leakage Current: Moore’s Law Meets Static Power”, Computer,
Dec. 2003, pp. 68-75.
[31]: Bohr M., Mistry K., Smith S., “Intel Demonstrates High-k + Metal Gate Transistor
Breakthrough in 45 nm Microprocessors,”, Intel, Jan. 2007,
http://download.intel.com/pressroom/kits/45nm/Press45nm107_FINAL.pdf
[32]: Tyson M., Intel confirms that its first 10nm chips will roll out in H2 2017, Hexus, Febr. 19 2016,
http://hexus.net/tech/news/cpu/90674-intel-confirms-first-10nm-chips-will-roll-h2-2017/
[33]: Jan C-H., RF CMOS Technology Scaling in High-k/Metal Gate Era for RF SoC (System-on-Chip)
Applications, IEDM’10 San Francisco, Dec. 2010, http://www.intel.com.br/content/dam/
doc/technology-brief/32nm-soc-with-rf-cmos-technology-presentation.pdf
[34]: Aktualisierte Fertigungsverfahren-Roadmap: GlobalFoundries & TSMC bei 14nm/16nm fast
zeitgleich, 3DCenter, Sept. 12 2014, http://www.3dcenter.org/news/aktualisierte-
fertigungsverfahren-roadmap-globalfoundries-tsmc-bei-14nm16nm-fast-zeitgleich

## Slide 116
6. References (5)
[35]: Moammer K., Samsung and Globalfoundries Beat TSMC to FinFETs – What This Means For
AMD, Nvidia and Intel, WCCF Tech, Dec. 19 2014,
http://wccftech.com/samsung-globalfoundries-tsmc-finfet-production/
[36]: Howse B., Smith R., Tick Tock On The Rocks: Intel Delays 10nm, Adds 3rd Gen 14nm Core
Product "Kaby Lake„, AnandTech, July 16 2015,
http://www.anandtech.com/show/9447/intel-10nm-and-kaby-lake
[37]: Intel's (INTC) CEO Brian Krzanich on Q2 2015 Results - Earnings Call Transcript, Seeking
Alpha, July 15 2015, http://seekingalpha.com/article/3329035-intels-intc-ceo-brian-
krzanich-on-q2-2015-results-earnings-call-transcript?page=2
[38]: Exynos 8 Octa (8890), Samsung, 2016,
http://www.samsung.com/semiconductor/minisite/Exynos/w/solution/mod_ap/8890/
[39]: Stein M. E., The Korean War: A Pacifist History, Pacifisn for the 21st Century, 21 January
2016, http://pacifism21.org/the-korean-war-a-pacifist-history
[40]: Korean War Fast Facts, CNN Library, June 21, 2016,
http://edition.cnn.com/2013/06/28/world/asia/korean-war-fast-facts

## Slide 118
RF CMOS Technology Scaling in High-k/Metal Gate Era for RF SoC (System-on-Chip) Applications Chia-Hong
Jan IEDM ’10, San Francisco 2010
http://www.intel.com.br/content/dam/doc/technology-brief/32nm-soc-with-rf-cmos-technology-presentation.pdf

## Slide 119
Several thousand people have been working on this project now for more than two years. This is the largest GPU endeavor, the largest chip processor endeavor, in the history of humanity. The R&D budget was several billion dollars,” Huang said.
At the DreamHack gamer gathering in Austin, Texas Friday night
NVIDIA CEO Jen-Hsun Huang unveiled the Pascal GPU based
GeForce GTX 1080 and said
[206]: NVIDIA CEO Jen-Hsun Huang Unveils GeForce GTX 1080, World’s Most Advanced GPU,
NVIDIA blog, May 06 2016, https://blogs.nvidia.com/blog/2016/05/06/geforce-gtx-1080/

## Slide 120
http://hvg.hu/tudomany/20160429_windows_10_mobile_windows_phone_eladasok_microsoft_surface_phone_megjelenese